A Field Effect Transisitor Synthesized using Multiple Al doped ZnO nanorods

Manoj Kumar1, Vijay Kumar Lamba2

1Research Scholar, I.K. Gujral Punjab Technical University, Kapurthala, Punjab (India)

2Global College of Engineering & Technology, Kahanpur Khui, Punjab (India)

1manoj10276@gmail.com

2lamba_vj@hotmail.com

Fig. 1: Wurtzite structure of ZnO

Source	         Drain

SiO2

SiO2

N++ Si Wafer

P - Substrate

ZnO nanorod

Fig. 2: SiO2 based ZnO nano FET

Table 1: Gate Voltage (V) Vs Drain Current, ID (A) for single nanorod each used in three ZnO nano FETs

| Gate Voltage (V) | -3 | -2 | -1 | 0 | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Drain Current (A) (FET 1) | 2x10-7 | 1x10-7 | 1.35x10-7 | 1.55x10-7 | 1.73x10-7 | 1.76x10-7 | 1.79x10-7 | 1.82x10-6 |
| Drain Current (A) (FET 2) | 2.5x10-7 | 1x10-7 | 1.35x10-7 | 1.55x10-7 | 1.65x10-7 | 1.7x10-7 | 1.75x10-7 | 1.8x10-7 |
| Drain Current (A) (FET 3) | 3x10-7 | 1.05x10-7 | 1.4x10-7 | 1.6x10-7 | 1.65x10-7 | 1.72x10-7 | 1.72x10-6 | 1.75x10-6 |

Fig. 3: Drain current versus gate-source voltage (ID -VGS) for (a) a single ZnO nanorod FET (b) two single ZnO FETs (c) Three single ZnO nanorod FETs

Table 2: Gate-source voltage,VGS versus drain current, ID at different values of drain-source voltage,VDS for a ZnO FET containing a single nanorod

| For VDS = 0V |  | For VDS = 0.4V |  | For VDS = 0.8V |  | For VDS = 1.2V |  | For VDS = 1.6V |  | For VDS = 2V |  | For VDS = 2.4V |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) |
| -1.5 | 0.00E+00 | -1.5 | 8.00E-09 | -1.5 | 3.00E-08 | -1.5 | 4.00E-08 | -1.5 | 4.40E-08 | -1.5 | 4.50E-08 | -1.5 | 4.70E-08 |
| -1 | 0.00E+00 | -1 | 1.00E-07 | -1 | 1.65E-07 | -1 | 2.00E-07 | -1 | 2.35E-07 | -1 | 2.50E-07 | -1 | 2.60E-07 |
| -0.5 | 0.00E+00 | -0.5 | 1.80E-07 | -0.5 | 3.50E-07 | -0.5 | 4.50E-07 | -0.5 | 5.00E-07 | -0.5 | 5.40E-07 | -0.5 | 5.60E-07 |
| 0 | 0.00E+00 | 0 | 2.80E-07 | 0 | 5.00E-07 | 0 | 6.50E-07 | 0 | 7.50E-07 | 0 | 8.20E-07 | 0 | 8.50E-07 |
| 0.5 | 0.00E+00 | 0.5 | 4.00E-07 | 0.5 | 7.00E-07 | 0.5 | 9.00E-07 | 0.5 | 1.03E-06 | 0.5 | 1.12E-06 | 0.5 | 1.18E-06 |
| 1 | 0.00E+00 | 1 | 5.30E-07 | 1 | 9.00E-07 | 1 | 1.15E-06 | 1 | 1.30E-06 | 1 | 1.42E-06 | 1 | 1.50E-06 |
| 1.5 | 0.00E+00 | 1.5 | 7.00E-07 | 1.5 | 1.10E-06 | 1.5 | 1.35E-06 | 1.5 | 1.55E-06 | 1.5 | 1.70E-06 | 1.5 | 1.80E-06 |

Table 3: Gate-source voltage,VGS versus drain current, ID at different values of drain-source voltage,VDS for a ZnO FET containing 10 nanorods

| For VDS = 0V |  | For VDS = 0.4V |  | For VDS = 0.8V |  | For VDS = 1.2V |  | For VDS = 1.6V |  | For VDS = 2V |  | For VDS = 2.4V |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) |
| -1.5 | 0.00E+00 | -1.5 | 8.00E-08 | -1.5 | 3.00E-07 | -1.5 | 4.00E-07 | -1.5 | 3.50E-07 | -1.5 | 4.50E-07 | -1.5 | 4.00E-07 |
| -1 | 0.00E+00 | -1 | 1.00E-06 | -1 | 1.65E-06 | -1 | 2.00E-06 | -1 | 2.35E-06 | -1 | 2.50E-06 | -1 | 2.60E-06 |
| -0.5 | 0.00E+00 | -0.5 | 1.80E-06 | -0.5 | 3.50E-06 | -0.5 | 4.50E-06 | -0.5 | 5.00E-06 | -0.5 | 5.40E-06 | -0.5 | 5.60E-06 |
| 0 | 0.00E+00 | 0 | 2.80E-06 | 0 | 5.00E-06 | 0 | 6.50E-06 | 0 | 7.50E-06 | 0 | 8.20E-06 | 0 | 8.50E-06 |
| 0.5 | 0.00E+00 | 0.5 | 4.00E-06 | 0.5 | 7.00E-06 | 0.5 | 9.00E-06 | 0.5 | 1.03E-05 | 0.5 | 1.12E-05 | 0.5 | 1.18E-05 |
| 1 | 0.00E+00 | 1 | 5.30E-06 | 1 | 9.00E-06 | 1 | 1.15E-05 | 1 | 1.30E-05 | 1 | 1.42E-05 | 1 | 1.50E-05 |
| 1.5 | 0.00E+00 | 1.5 | 7.00E-06 | 1.5 | 1.10E-05 | 1.5 | 1.35E-05 | 1.5 | 1.55E-05 | 1.5 | 1.70E-05 | 1.5 | 1.80E-05 |

Table 4: Gate-source voltage,VGS versus drain current, ID at different values of drain-source voltage,VDS for a ZnO FET containing 20 nanorods

| For VDS = 0V |  | For VDS = 0.4V |  | For VDS = 0.8V |  | For VDS = 1.2V |  | For VDS = 1.6V |  | For VDS = 2V |  | For VDS = 2.4V |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) |
| -1.5 | 0.00E+00 | -1.5 | 1.50E-07 | -1.5 | 3.75E-07 | -1.5 | 7.20E-07 | -1.5 | 1.05E-06 | -1.5 | 1.35E-06 | -1.5 | 1.65E-06 |
| -1 | 0.00E+00 | -1 | 9.00E-07 | -1 | 1.90E-06 | -1 | 2.85E-06 | -1 | 3.60E-06 | -1 | 4.20E-06 | -1 | 4.65E-06 |
| -0.5 | 0.00E+00 | -0.5 | 2.00E-06 | -0.5 | 4.00E-06 | -0.5 | 5.70E-06 | -0.5 | 7.20E-06 | -0.5 | 8.34E-06 | -0.5 | 9.30E-06 |
| 0 | 0.00E+00 | 0 | 3.45E-06 | 0 | 6.90E-06 | 0 | 9.60E-06 | 0 | 1.19E-05 | 0 | 1.35E-05 | 0 | 1.50E-05 |
| 0.5 | 0.00E+00 | 0.5 | 6.00E-06 | 0.5 | 1.07E-05 | 0.5 | 1.43E-05 | 0.5 | 1.71E-05 | 0.5 | 1.92E-05 | 0.5 | 2.10E-05 |
| 1 | 0.00E+00 | 1 | 9.00E-06 | 1 | 1.50E-05 | 1 | 1.94E-05 | 1 | 2.28E-05 | 1 | 2.52E-05 | 1 | 2.70E-05 |
| 1.5 | 0.00E+00 | 1.5 | 1.35E-05 | 1.5 | 2.10E-05 | 1.5 | 2.55E-05 | 1.5 | 2.85E-05 | 1.5 | 3.09E-05 | 1.5 | 3.27E-05 |

Fig. 4: Drain-Source Voltage, VDS Vs Drain Current, ID characteristics (VDS - ID) of (a) ZnO nanorod FET containing a single nanorod, (b) ZnO nanorod FET containing 10 nanorods, and (c) ZnO nanorod FET containing 20 nanorods.

Table 5: Gate-source voltage, VGS versus drain current, ID (VGS - ID) for ZnO FET containing different number of nanorods

| For a single nanorod |  | For 10 nanorods |  | For 20 nanorods |  |
| --- | --- | --- | --- | --- | --- |
| VGS (V) | ID (A) | VGS (V) | ID (A) | VGS (V) | ID (A) |
| -4 | 3.75E-06 | -4 | 3.75E-06 | -4 | 3.75E-06 |
| -3 | 3.00E-06 | -3 | 3.00E-06 | -3 | 3.00E-06 |
| -2 | 9.50E-06 | -2 | 2.38E-06 | -2 | 2.63E-06 |
| -1 | 1.40E-06 | -1 | 1.88E-06 | -1 | 1.25E-05 |
| 0 | 1.70E-06 | 0 | 2.00E-05 | 0 | 1.90E-05 |
| 1 | 1.85E-06 | 1 | 2.30E-05 | 1 | 2.38E-05 |
| 2 | 1.95E-06 | 2 | 2.43E-05 | 2 | 2.63E-05 |
| 3 | 2.00E-06 | 3 | 2.50E-05 | 3 | 2.70E-05 |
| 4 | 2.03E-06 | 4 | 2.54E-05 | 4 | 2.75E-05 |

Fig. 5: Gate-source voltage, VGS versus drain current, ID (VGS - ID) for ZnO FET containing 1, 10 and 20 nanorods

Fig. 6: On – Off Current versus number of nanorods used in ZnO FETs